Conbextra EP300 DP

High strength, flowable, low exotherm, three-part epoxy resin grout for large volume pours in dynamic / repetitive load applications - gaps up to 300mm

1.0 	Grouting Requirements

  - To the nominated area(s) (specify details and areas of application), grouting must be carried out using a 	high strength, flowable, low exotherm, epoxy resin grout, suitable for dynamic /repetitive load 	applications, and suitable for grouting gaps up to 300mm.

  - The three-component pack is to be stored, handled and placed, strictly in accordance with the 	manufacturer’s current technical data sheet and instructions.

  - The hardened epoxy resin grout shall exhibit the following properties at 23oC:

| Compressive strength (AS1478.2 2005): | 65 MPa @ 1 day |
| --- | --- |
|  | 85 MPa @ 7 days |
|  | 90 MPa @ 28 days |
| Indirect Tensile Strength (AS1012.2.10-2000): | 14 MPa @ 28 days |
| Flexural Strength (AS1012.2.11-2000): | 33 MPa @ 28 days |
| Modulus of Elasticity (AS1020.17-1997): | 16 GPa |
| Creep 28 days @ 2.8 MPa (ASTM C1181-00): | @ 60°C 4.47 x 10-3 cm/cm |
| Flow (AS 1478.2) | 500mm |

  - Fosroc Conbextra EP300 DP meets the performance criteria and is approved for this application