Dekguard® O

**High performance, translucent aliphatic acrylic, chloride ion and carbonation protective coating for concrete and masonry**

**1.00 Protective Coating System**

**1.10 Concrete / Masonry Surfaces**

1.11 All surfaces to receive the coating system should be dry and free from contamination such as oil, grease, loose particles, decayed matter, moss, algal growth, laitance, and all traces of mould release oils and curing compounds.

**1.20 Coating System**

1.21 The protective coating shall comprise a penetrating silane-siloxane primer a single component aliphatic solvent based acrylic coating.

1.22 The silane-siloxane primer should be applied in one or more coats until the recommended application rate of 0.4 litres /m2 has been achieved.

1.23 The protective coating should be applied in two coats to achieve a total dry film thickness of not less than 150 microns.

When tested to AS/NZS 4548.5-1999 the coating shall exhibit a Carbon dioxide diffusion resistance >350m equivalent thickness of air (R) and Chloride ion diffusion coefficient: 0.1 x 10-12m²/sec @ 218 days. .

**1.30** **Fosroc Dekguard O** applied in conjunction with **Dekguard Primer** meets the performance criteria and is approved.

Mar-07

Mar-07