Concure CR

Chlorinated rubber based concrete curing compound

1.00	Concrete Curing Compound

1.10	Concrete Surface

1.11	The curing compound should not be applied to soft, wet concrete or render surfaces which will be 	disturbed and prevent formation of the curing film.

1.12	To those nominated floor areas requiring a curing compound, ensure the concrete surface is completely 	free of stains, oils, form coatings, etc., to obtain good adhesion of the curing compound, and to avoid 	obtaining discoloration or uneven surface effects.

1.20	Curing Compound

1.21	The curing compound is to be applied evenly over the freshly laid concrete as soon as possible after 	final trowelling, just after the disappearance of the surface bleed water for maximum water retention, 	(approximately 1-2 hours depending on the ambient temperature and atmospheric conditions) strictly in 	accordance with the manufacturer’s instructions and current technical data sheet.

1.22	The curing compound is to be based on chlorinated rubber. All designated areas are to have a liquid 	curing compound applied in a single coat to achieve a total dry film thickness of not less than 35 	microns. The curing compound is to provide the following properties:

| Volume solids content: | >18% |
| --- | --- |
| Water retention efficiency AS3799: | >90% |

1.30	Fosroc Concure CR meets the performance criteria and is approved.