Proofex® Torchseal A600

**3.0mm thick reinforced polymer modified bitumen torch-on waterproofing membrane**

**1.00 Polymer modified bituminous waterproofing membrane**

Where so designated on the drawing, the surfaces shall be covered with a 3.0mm thick torch applied, polyester reinforced, polymer modified bituminous waterproofing membrane.

 Application of the membrane should be carried out by a competent applicator, well trained in the application of modified bitumen torch applied membrane systems

**1.10 Surface Preparation**

 All surfaces receiving the waterproofing membrane must be firm, dry, and free from contaminants and loose material. Surfaces must also be even and smooth, without any defects that could damage the membrane. Rough concrete must be “faired up” before commencing application.

 Priming is essential to ensure adhesion of the membrane – refer to the manufacturer’s product data sheet for guidance.

**1.20 Bituminous Waterproofing Membrane**

 The waterproofing membrane shall be 3.0mm thick, reinforced with non-woven polyester fabric and be based on an elasto-plastomeric bitumen-polymer compound.

 The waterproofing membrane shall be independently tested to and comply with the requirements of AS/NZS 4654.1:2012 Waterproofing membranes for external above-ground use Part1:Materials.

 The waterproofing membrane shall exhibit the following properties:

|  |  |
| --- | --- |
| **Thickness:** | 3mm (±5%) |
| **Flow resistance at elevated temperature (EN 1110):** | ≥ 120°C |
| **Flexibility at low temperature (EN 1109):** | ≤ minus 10°C |
| **Tensile strength (EN 12311-1) N/50 mm:** | longitudinal: 700 (±20%)transverse: 450 (±20%) |
| **Tensile elongation (EN12311-1):** | longitudinal: 40% (±15%)transverse: 45% (±15%) |
| **Dimensional stability (EN1107-1):** | ≤0.5% |
| **Resistance to tearing (EN12310-1):** | longitudinal: 150 N (±30%)transverse: 160 N (±30%) |
| **Impermeability to water (EN1928 B method):** | ≥ 60 kPa |

.

1.11 The waterproofing membrane shall be applied in accordance with the manufacturer’s product data sheet.

**1.20** **Fosroc Proofex Torchseal A600** meets the performance criteria and is approved.

Mar-07

Mar-07